## Slide 1
Contrast Variation in elastic
Neutron Scattering
At small angles
Philipp Gutfreund
ILL, Grenoble, France
gutfreund@ill.eu
Uppsala University, October 6, 2020

## Slide 2
_________________________________
Giovanna Fragneto HERCULES 2012

## Slide 3: Outline
  Fundamental Scattering Theory
  Small Angle Neutron Scattering (SANS)
  Reflection of Neutrons at small angles (NR)
  NR Instrumentation and Data Reduction
  NR Data analysis + Practical (start at 13:30)

## Slide 4: 1. Fundamental Scattering Theory

## Slide 5: Elastic differential cross section
No inelastic scattering considered:
Out of the direct beam:
Alternative:
Fermi’s golden rule:
Notes: The quantity measured in a scattering experiment is the differential cross section.
If we build the absolute square of the probability function and ignore cross terms of the direct and scattered beams (no multiple scattering) we end up with the absolute square of the scattering function as the resulting cross section out of the direct beam.

## Slide 6: 1st order Born Approximation
Inhomogeneous Helmholtz equation:
Ansatz:
Scattering function:
Assumptions:
Wave is the same inside and outside of the sample (kinematic approximation)
Interaction potential is small (perturbation theory)
Single scattering event (1st order)
Neutron and X-ray scattering on a potential much smaller than the wavelength results in radial waves!
Notes: The wave vector in the Angstrom range, the interaction potential is in the fm range, thus small. Common between neutrons and X-rays is the wavelength. The scattering function is the Fourier transformation of the potential V.

## Slide 7: 2nd order Born Approximation?
Scattering function f(2) (for particles):

## Slide 8: Potential V(r) for a single nucleus
Cold neutron wavelengths on Å length scale
Scattering on nuclei (strong interaction) of fm size
Point scattering
Scattering function:
Scattering Function of a single nucleus is described by a single number!
Definition of scattering length b:
Fermi pseudo potential:
Notes: Scattering on a single point.

## Slide 9
Origins of scattering differ for the different methods.
X-rays dominated by number of electrons:
Neutrons rely on contrast of nucleus: similar for many different elements, but show strong variations from different isotopes of same element, especially hydrogen.
Scattering cross sections for neutrons and X-rays

## Slide 11: Neutron-matter interaction
Neutron-nucleus
Neutron-magnetic field
Neutron-magnetisation
Interaction neutron-nucleus
  Isotropic and ponctual
Zeeman interaction
  Neutron spin – magnetic field
Pauli spin matrix
nuclear magneton
g-factor
permeability
Neutrons only see the magnetization perpendicular to the scattering vector!
Notes: The Fourier-transformed magnetization of the sample M|| is the component in-plane of the surface (for NR) (but perpendicular to q)!

## Slide 12: Comparison nuclear and magnetic neutron scattering lengths.

## Slide 13: Spin scattering
Pure nuclear scattering:
Fermi Golden rule:
Nuclear scattering is entirely non-spin-flip.
Non-spin-flip scattering is sensitive to magnetization parallel to neutron spin.
Spin-flip scattering is sensitive to magnetization perpendicular to neutron spin.
Notes: If we do the calculations we see that the spin incoherent scattering adds with a factor of 1/3 to the total incoherent scattering. (R. Stuart script)

## Slide 14: Coherent/Incoherent Scattering
Spin-incoherence:
Neutron Spin:
Neutron+
(random) nucleus spin:
Probability
Average (coherent) scattering length:
Strandard variation (incoherent) scattering length:
Same for natural distribution of isotopes (isotope incoherence)
Total cross section:

## Slide 15: Neutron Scattering Cross Sections
Scattering at nuclei
Typical Wavelengths (cold neutrons) 2 Å - 30 Å
No charge, thus deeply penetrating matter
Possible contrast tuning by exchanging isotopes, especially Protons with Deuterons
Notes: Some elements like oxygen have no incoherent scattering due to the absence of a nuclear spin and isotopes.

## Slide 16: 2. Small Angle Neutron Scattering (SANS)
Porcar et al.

## Slide 17
● colloidal suspensions
● polymers:
chains, blends , block copolymers
● surfactant assemblies
● biological molecules:
proteins, nucleic acids, complexes, small bio-related molecules
● surface properties of catalysts
● metal physics:
phase stability of alloys, precipitates, interfaces, grain boundaries
● materials science:
structural tailoring and testing, stability under load
● nanocrystalline materials:
grain size, interface, porosity, magnetic nanostructures
● flux lines in superconductors
Applications of SAS

## Slide 18: Scattering length density
For small angle scattering the positions of individual atoms are not resolved,
Therefore the mean scattering length density (SLD) Nb is seen:
Optical refractive index:
Absorption coefficient
SLD
Neutrons:
X-rays:
Neutron, X-rays and light scattering at small angles
can be described by the scattering on an optical potential!
SLD:
Nb = ρ0*b
Notes: But, the refractive index is smaller than 1 in most cases: Total external reflection!
The SLD is wavelength independent. Show imaginary SLD. Uebung: n Selber ausrechen (Doktorarbeit S.28).

## Slide 19: Scattering Function from an assembly of particles
Particle form factor
Particle structure factor
Difference of length scattering density
between particle and solvent
Volume of individual
particle
Volume fraction
of particles
The scattered intensity per unit volume V of an assembly of isotropic scatterers of individual volume Vp and volume fraction F is:
Notes: The convolution theorem FT( int f(x)g(x-x1) dx)=FT(g(q))*FT(f(g)). Thus we can factorize the structure and form factors.

## Slide 20: Scattering from Polymer melts
SANS from mixture of deuterated and protonated polymers:
SLD difference between deuterated and protonated monomers
With deuteration SANS can see individual polymer chains in an entangled melt!
Polymerization
Debye function
Fraction of deuterated molecules
PDMS melt
Monomer volume
Isotropic scattering
Kawecki et al., Sci. Rep., 9, 1-6 (2019).
1/RG
Notes: Scattering on an assembly of points. I show a structure factor of a liquid here, as an example.

## Slide 21: Scattering Function for Polymers
Diffracted Intensity from N particles:
For Gaussian polymers:
Scattered intensity proportional to FT of the Auto-correlation!
R.G. Kirste & W.A. Kruse, Polymer 16, 120 (1975)
D.G.H. Ballard et al., Eur. Polymer J. 9, 965 (1973)
Auto-correlation function (Patterson function)
Debye function:
Radius of gyration:
For Gaussian chains this the Debye function.
Notes: Scattering on an assembly of points. I show a structure factor of a liquid here, as an example.

## Slide 22
Do chains in solution deform under shear?
Yes, they elongate along the flow (slightly)
static
flow direction
30 wt% Polystyrene (PS Mn=520 kg/mol) in d-toluene:
Wi = 210 s-1 * 0.14 s = 30
Wi * Ne/N = 30 / 10 = 3
At PAXY/LLB
neutral direction y
Rg∥/Rg⟂ = 1.07
Korolkovas et al., Soft Matter, 15, 371 (2019).
shear
Anisotropic scattering

## Slide 23
The deformation is non-affine below 8 nm at Wi=30. (Blob size 1nm, Rg=27 nm)
This is roughly the tube diameter!
Korolkovas et al., Soft Matter, 15, 371 (2019).
Single chain form factor:
(Eq. 20)
MSD
Do chains in solution deform under shear?

## Slide 24
Coarse-grained polymer solution
concentration c and molecular weight Mw
De Gennes Scaling concepts in polymer physics. Cornell university press, 1979.
Doi & Edwards The Theory of Polymer Dynamics. Oxford university press, 1989.
Number of blobs
Blob size
Average contrast of the solution
Contrast between polymers

## Slide 25
General behaviour of a scattering curve
log(q)
log(I)
Molecular mass
Concentration
Dr2
q-n
n=1: cylinder, 1D
n=2: disk, 2D
Interface
(q-4)
Guinier
range
(radius of gyration)
Local structure
Analytical expressions for spheres, cylinders, ellipsoids, disks, muli-shell particles, Gaussian coils, …
Case of a dilute solution of uncorrelated particles
Guinier analysis
(model independent):
Slope = RG2 / 3
1.3/RG
2π/d

## Slide 26
Analytical expressions of form factors
Sphere
Disk/cylinder
Ellipsoid
Multi-shell

## Slide 27
Polydispersity
Case of polydisperse spherical particles without interaction
Log-normal distribution
R = 90 Å

## Slide 29
Combined effect of polydispersity and resolution
Favor the resolution rather than the flux
Importance of the instrumental resolution in the data treatment
More details… Effect of instrumental resolution and polydispersity on ideal form factor in SANS, I. Grillo, ILL Technical Report, 2001, ILL01GR08T

## Slide 30
Polydispersity in size
(log-normal distribution)
Instrument resolution
Form Factor
Pedersen (Adv. Colloid Interface Sci. 1997, 70, 171)
Nallet et al.( J. Phys. II France, 1993, 3, 487)
Structure Factor
Percus-Yevick (Phys. Rev. 1958, 110, 1 )
Hayter-Penfold (Mol. Phys. 1981 42,109)
(
)
(
)
(
)
(
)
dq
dr
q
r
P
r
r
G
q
q
q
R
r
q
I
o
o
o
o
o
ú
û
ù
ê
ë
é
D
=
ò
ò
¥
¥
0
0
exp
,
,
,
,
,
,
s
S (q)
Summary

## Slide 31: Break 15 min

## Slide 32: 2. Small Angle Neutron Scattering (SANS) Applications

## Slide 33
SAS techniques
Small angle neutron scattering
PAXY, Laboratoire Léon Brillouin, Saclay
l = 12 Å, D = 5 m l = 4 Å, D = 5 m and 1 m 0.0047 < q (Å-1) < 0.45
Probe the size and polydispersity of liposomes

## Slide 34
Size and shape of the liposomes
10-4
10-2
1
102
104
0.001
0.01
0.1
1
q (Å-1)
I (cm-1)
Pure liposome
DOTAP/DOPE = 4.2 10-2 mol/l
Charged liposome
DOTAP/DOPE = 4.2 10-2 mol/l
X LCOB =0.5
tc = 26.0 Å
th = 5.4 Å
e = 38.8 Å
Ro = 445 Å
s = 0.13 Å
ρc,n = -1.29 109 cm-2
ρh,n =3.5 1010 cm-2
tc = 24.0 Å
th = 10.0 Å
e = 44.0 Å
Ro = 459 Å
s = 0.18 Å
ρc,n = 2.61 109 cm-2
ρh,n =5.46 1010 cm-2

## Slide 35
Cholesterol Exchange
Cholesterol
+ D-lipids
H-lipids
Lipid Exchange
D-lipids
H-lipids
H2O
D2O
Advantages:
In-situ transfer by Time-Resolved SANS
t = 0
t = inf
Do not require vesicles isolation (in situ technique)
No need of fluorescent or tag cholesterol
Access early stage of transfer
Accurate control on lipid membrane composition and structure
Can be applied to anything (just require deuterated materials)
Arenas et al., Sci. Rep., 7, 45875 (2017).

## Slide 36
PSS
+ PEDOT
Functionalized Gold Nanospheres
Au
Contrast SLD [* 10-6 Å-2]
Low-q intensity [a.u.]
D2O
AuMW
ZAC
H2O
SLDs:
D2O = 6.3 * 10-6 Å-2
AuMW = 4.66 * 10-6 Å-2
ZAC = 3 * 10-6 Å-2
PSS/PEDOT = 2 * 10-6 Å-2
H2O = -0.57* 10-6 Å-2
24.2 nm
≈3 nm
50%
water

## Slide 37
EO20PO70EO20
Materials and method
TEOS silica precursor : Si-(RO)4
Hydrolysis and condensation
RO
Si
OR
OR
OR
R= -CH2CH3
P123
EO = -CH2-CH2-O-
PO = -CH2-CH(CH3)-O-
r0
r2
r1
r0
r1
r2
r(r)
r(r)
Neutron
RX

## Slide 38
Micellar solution
Precipitation after 22 min

## Slide 39: Evolution of the micellar shape before precipitation
Spherical micelles before TEOS addition
R2 = 4 nm, R1 = 7.1 nm and b = 0.26.
Cylindrical micelles after 15 minutes
R2 = 2.9 nm, R1 = 6.9 nm, L = 22 nm and b = 0.4
Core-shell models for sphere and cylinder
F(q,R) is the form factor of a sphere or cylinder

## Slide 40
In-situ study of the synthesis of mesoporous materials
1M. Imperor-Clerc, 2I. Grillo, 3A.Y. khodakov, 4D. Durand, 5V.L. Zholobenko
Chem. Commun. 2007 (8) 834-836
1 LPS, Université Paris Sud, Orsay, F;2 I.L.L, F; 3 UCCS, Université des Sciences et technologies de Lille, F; 4 IBBMC, Université Paris-Sud, F; 5 Dpt of Chemistry, Keele, UK
hybrid material
surfactant + silica
solution oligomers
calcination (400°C)
Catalysis supports, filtration membranes, surface treatment (glass industry), confinement of liquids …
Nano-particles inside the porosity :(metallic, metallic oxydes, semiconductors)
New material properties : optical, magnetic …

## Slide 41
Usefull references
Theory
● A. Guinier, G, Fournet (1955) Small angle scattering of x–rays. Wiley, New York
● H. B. Stuhrmann, J. Appl. Cryst (1974), 7, 173-178
● Neutron, X-rays and Light: Scattering Methods applied to soft condensed Matter, ed. P. Lindner and T. Zemb, Elsevier, 2002,
● D. Lairez, J. Peta J. Phys IV, 130 (2005) 39-62
Model and data analysis
● O. Glatter, Acta Phys. Austriaca (1977), 47, 83-102, J. Appl. Cryst. (1977),10, 415-421; J. Appl. Cryst. (1980),13, 7-11
● D. I. Svergun, M.H.J. Koch, Rep. Prog. Phys. (2003), 66, 1735-1782
● J.B. Hayter, J. Penfold, Molecular Physics (1981), 42, 109-118
● J. Pedersen Adv. Colloid Interface Sci. (1997), 70, 171-210
Google NIST SANS tutorials + SANS Toolbox (B.Hammouda)!!

## Slide 42: 3. Small Angle Reflectometry

## Slide 43: Applications of Neutron Reflectometry
Magentism: Magneitc multilayers, Thin magnetic films, Thin film magnetometry
Layer-by-Layer

## Slide 44: Exact solution of step potential (QM)
Helmholtz equation:
Complete Solution:
Fresnel functions:
Notes: We can completely solve this problem and calculate the transmission functions of the incoming and reflected waves.
Here I used the z-axis projection.

## Slide 45: Reflectometry (Optics)
Snellius:
Fresnel:
For an ideal smooth interface (Fresnel-reflectivity):
Total Reflection :
For q >> qc:

## Slide 46: Total Reflection
For both kinds of radiation the refractive index is a function of the scattering length density and wavelength.
As with light, total reflection may occur when neutrons pass from a medium of higher refractive index to one of lower refractive index.
Total Reflection of neutrons was first observed in 1944 by Fermi and Zinn (Phys. Rev. 70, 103 (1946))

## Slide 47: Roughness
  Roughness at the molecular level : interdiffusion between the layers, x < 10 nm.
  Intermediate roughness (0.01 µm < x < 50 µm).
  A large scale roughness (beam size > x > 50 µm).

## Slide 48: Roughness
In the Born approximation (validity: |σqz|<<1):
Gaussian roughness:
Nevot-Croce:
Born approximation:
Exact optical solution
(no in-plane correlation):
L.G. Parratt, Phys. Rev. 95, 359 (1954).
Névot and Croce, Revue Phys. Appl. 15, 761 (1980).
Notes: Nevot-Croce for uncorrelated molecular/atomic roughness.

## Slide 49: The Fresnel reflectivity + Roughness
For roughness σ:
For an ideal smooth interface:
Notes: This results in the exact Reflectivity as Emanuel told us yesterday.

## Slide 50: The Fresnel reflectivity + Roughness
For qz » qc :
For an ideal smooth interface:
X-ray reflection from
free water surface
Deviation due to capillary waves!

## Slide 51: Stratified Medium (Matrix method)
Refraction matrix
(Through continuity
at interfaces):
F. Abelès, J. de Physique et le Radium 11, 307 (1950).

## Slide 52: Stratified Medium (Matrix method)
Transition matrix:
Transfer matrix:
Notes: We can completely solve this problem and calculate the transmission functions of the incoming and reflected waves.
Here I used the z-axis projection.

## Slide 53: Stratified Medium (Matrix method)
reflection coefficient:
If subphase is sufficiently thick (>0.1 mm):

## Slide 54: Interference
The neutrons are partially reflected and transmitted:
ki
k2
0
k1
0
2
0
2
1
1
k1
0
1675 - Newton realised that the colour of the light reflected by a thin film illuminated by a parallel beam of white light could be used to obtain a measure of the film thickness. Spectral colours develop as a result of interference between light reflected from the front and back surfaces of the film.
1931 - H. Kiessig measures the total external reflection of X-rays and the thickness interference oscillations named after him. (Ann. d. Physik 402, 715)

## Slide 55: Reflectometry from stratified media
Recursively calculating the reflected and transmitted intensity via Fresnel adding the Debye-Waller roughness leads to the reflectivity of layered systems.
L.G. Parratt, Phys. Rev. 95, 359 (1954).

## Slide 56: Reflectometry from stratified media
2π/d

## Slide 57: Break 15 min

## Slide 58: 3. Small Angle Reflectometry Applications

## Slide 59: Model Cell Membranes

## Slide 60
Model structure of lipid membrane
= layered model of structure & composition
z
Log R
Neutron wavelength << light wavelength
nanothin films e.g. lipid membranes (~ 5nm)
Solid = Si-SiO2
liquid = D2O/H2O
Scattering length density profile (z)
= neutron refractive index profile
SiO2
D2O
Optical Matrix modeling
Reflectometry

## Slide 61
Scattering length density profile (z)
= neutron refractive index profile
Log R
h-lipid
d-lipid
z
thickness
ρ(z)
ρ
SiO2
D2O
Model structure of lipid membrane
= layered model of structure & composition
z
Solid = Si-SiO2
liquid = D2O/H2O
Reflectometry
Notes: The contrast between the water phase (D2O) and the lipid bilayer can be tuned by (partially) deuterating the lipid.

## Slide 62
Scattering length density profile (z)
= neutron refractive index profile
Model structure of lipid membrane
= layered model of structure & composition
Log R
SiO2
D2O
h-lipid
d-lipid
z
thickness
ρ(z)
ρ
z
Solid = Si-SiO2
liquid = D2O
Reflectometry

## Slide 63
Scattering length density profile (z)
= neutron refractive index profile
Model structure of lipid membrane
= layered model of structure & composition
z
Log R
h-lipid
d-lipid
z
thickness
ρ(z)
ρ
z
Solid = Si-SiO2
liquid = H2O
SiO2
D2O
Reflectometry

## Slide 64
Solid/liquid cell for adsorption on surfaces
Humidity chamber
SAMPLE ENVIRONMENT

## Slide 65
Cholesterol goes in the inner leaflet
GM1 enters the membrane
_________________________________
Giovanna Fragneto HERCULES 2012
Notes: GM1 (monosialotetrahexosylganglioside) studies have indicated that GM1 can ease the symptoms of Parkinson's disease

## Slide 66
Adsorption troughs for adsorption from solution
Langmuir trough for insoluble monolayers
SAMPLE ENVIRONMENT

## Slide 67
Courtesy H. Wacklin
Courtesy Hanna Wacklin
10s
2˚
PLA2 has a delay of 1.5h before hydrolysis begins
Monolayer s2 tructure at 2.0° measured in min – 20s possible.
PLA2 hydrolyses ~ 50% of d54DMPC monolayer and remains attached to it
PERSPECTIVES:
fast kinetics
Notes: Phospholipases A2 (PLA2s) are enzymes that cleave fatty acid (phospholipids) hydrolyzing the bond

## Slide 68
Co-polymer Langmuir monolayers
Barriers
Water contrast-matched
to CA/BP mixture
NbPBd = 5.72.10-6 Å-2 NbCA = 1.23.10-6 Å-2
water
PBd
PBd/CA
Structure of hydrophobic (polybutadiene)/ hydrophilic (cellulose acetate) polymer blend at the air/water interface.

## Slide 69
Polymer brush under shear
Grafting-to PS brush Mw = 82 kg/mol surface coverage = 0.16
Korolkovas et al., Macromolecules 50 (1215) 2017.
Grafted h-PS
d-PS in DEP

## Slide 70: Monomer density profile of ‘grafted from’ brush
Phase diagram of brushes in a melt matrix:
Dry brush!
Same, but larger interfacial width.
(300 Å)

## Slide 71: Flowing polystyrene on ‘grafted from’ brush
Phase diagram of brushes in a melt matrix:
dry brush
wet brush (parabolic density profile)!

## Slide 72
Results:
An atomically smooth interface has emerged in the contacting PS.
A depletion layer has to be assumed:
DTS: 4.2 ± 0.14 Å
OTS: 6.8 ± 0.08 Å
same density
Thin polystyrene films on SAMs
Gutfreund et al., Phys. Rev. E 87 (12306) 2013.

## Slide 73
What is the chemical composition of the depletion layer?
Neutron Reflectivity: deuterated PS on protonated SAM
The depletion layer incorporates a part of the SAM and the Polymer
The amount of deuterated and protonated material corresponds very well to the assumption of the phenyl ring ordering
Thin polystyrene films on SAMs
OTS interface layer consists of:
66 ± 4 % PS and 11 ± 3 % silane
DTS interface layer consists of:
32 ± 12 % PS and 43 ± 12 % silane.
Depletion layer is the result of an altered interfacial order.
Surface order is replicated in the adjacent polymer melt. (Reason for Slip?!)
Gutfreund et al., Phys. Rev. E 87 (12306) 2013.

## Slide 74: Watching thermoresponsive hydrogel take up water
Proronated poly(styrene-block-monomethoxydiethylenglycol-acrylate-block-styrene) (P(S-b-MDEGA-b-S)) films +D2O -huge contrast
Macromolecules zhong et. al.
46 4069 (2013)

## Slide 75: Experimental set-up
Guide field
polariser
flipper
sample
analyser
detector
flipper
B
+
-
+
-
+
-
-
+
M
4 cross-sections

## Slide 76: Polarized Reflectivity
For magnetization and external field (+neutron spin) parallel:
No spin-flip scattering
++ and -- reflections identical to non-magnetic reflectivity but with shifted critical edge according to magnetic scattering length

## Slide 77: Polarized Reflectivity
Notes: Show Zabarkshs data for perpendicular q B realtion

## Slide 78: Polarized Reflectivity
Another origin for an asymmetry in R-+ and R+- signals can be a very strong external field in conjunction with a strong spin-flip scattering due to the Zeeman effect.
In case of an arbitrary angle γ between M and B0 and an arbitrary final neutron spin angle (vector analysis) all four channels are different and non-zero.
Notes: This results in the exact Reflectivity as Emanuel told us yesterday.

## Slide 79: Polarized Reflectivity
In case of M perpendicular
to B0 both spin-flip channels
and non-spin-flip channels
are non zero and identical.
Notes: This results in the exact Reflectivity as Emanuel told us yesterday.

## Slide 80: Polarized Neutron Reflectivity
Allows the study of the magnetic configuration of a multilayer system: access to the magnetisation amplitude and direction in each layer.
  Determination of in-depth magnetic profiles
  Absolute measurement of the magnetic moment in µB (sum of the spin and orbital moment)
  But sensitivity only to the in-plane magnetic moment (and perpendicular to q).
  Resolution of the order of 0.1µB (better on simple systems)
  No sensitivity to the substrate para/dia-magnetism.
  No absorption, no phenomenological parameter, absolute normalisation.

## Slide 81: Ni layer corrosion
M. Wood et al., Langmuir 2015
SDS-
DTAB+
pH 2
pH 6

## Slide 82: Reflectometry from a multilayer
Closely related to Bragg condition in crystals,
but slightly shifted by the critical edge.
layer pair thickness
Bragg peak
order

## Slide 83: Polyelectrolyte multilayer (LbL)
Layer-by-Layer method (LbL):
Polymer Conformation:
Decher, G., Science (1997) 277, 1232-1237.
Zhang, H. N., and Rühe, J., Macromolecules (2005) 38, 10743-10749.
Specular Neutron Reflectivity (D17):
Individual layer pair thickness: 2.4 nm
C. Higy, G. Fragneto, ILL and G. Decher, Univ. Strasbourg
Scattering length density profile:
PAH/PSSd
3xPAH/PSSh

## Slide 84
  V. F. Sears 'Neutron Optics', Oxford Press, Oxford (1989)
  Lekner J 1987 in: “Theory of Reflection" Martinus Nijhoff Dordrecht
  Born M and Wolf E 1989 in: “Principles of Optics” Pergamon Press Eds. Oxford
  Penfold J and Thomas R K 1990 J. Phys. Condens. Matter 2 1369
  Russell T. P. 1990 Mat. Sci. Rep. 5 171
  Felcher G P 1981 Phys. Rev. B 24 1995
  Sinha S K, Sirota E B, Garoff S and Stanley H B 1998 Phys. Rev. B 38 2297
  Zhou X-L and Chen S-H 1995 Phys. Rep. 257 223
  W. Williams 'Polarized Neutrons' , Oxford Press, Oxford (1989)
  Névot L and Croce P 1990 Rev. de Phys. Appl. 15 761
  Daillant J and Gibaud A 1999 in:
  “X-ray and Neutron Reflectivity: Principles and Applications” Springer Eds.
  Heavens O S 1955 in: “Optical Properties of Thin Films”, Butterworths Eds. London
Some useful references:
Web-sites:
http://www.mrl.ucsb.edu/~pynn/ (Roger Pynn)
http://www.pcl.ox.ac.uk/~rkt/ (Bob Thomas)
Cubitt R. and Fragneto G. 2002 “Neutron Reflection: Principles and Examples of Applications”, in Scattering, p. 1198-1208, Academic Press eds.

## Slide 85: 4. NR Instrumentation and Data Reduction

## Slide 86: Two possible methods for neutrons
For a constant dq-resolution TOF is less efficient but if resolution can be relaxed to constant dq/q it is faster.
k
0
1
q
2
q
k
1
1
q
2
k
2
q

## Slide 87: D17 – Time-of-flight and monochromatic vertical sample reflectometer at ILL
http://www.ill.eu/instruments-support/instruments-groups/instruments/d17/
Q range=0.005 Å-1 < q < 4 Å-1
White flux=1010n/s/cm2
Polarized neutrons+He3
Vertical samples only

## Slide 88: Data reduction for monochromatic NR
Overillumination:
Footprint correction:
Raw Reflectivity:
R = I/I0
I: Counts in detector
I0: Direct beam intensity (attenuator used?)

## Slide 89: Two possible methods for neutrons
Since q = 4πsinθ/λ, reflectivity R(q) can be measured in two ways:
using a monochromatic beam and scanning the angle of incidence θ
using a polychromatic beam covering a range of q-values at any given θ
In practice, method 2 is useful a the range of q is measured simultaneously, which allows structural changes to be monitored as a function of time.

## Slide 90: Two possible methods for neutrons
Since q = 4πsinθ/λ, reflectivity R(q) can be measured in two ways:
using a monochromatic beam and scanning the angle of incidence θ
using a polychromatic beam covering a range of q-values at any given θ
In practice, method 2 is useful a the range of q is measured simultaneously, which allows structural changes to be monitored as a function of time.

## Slide 91: Two possible methods for neutrons
Since q = 4πsinθ/λ, reflectivity R(q) can be measured in two ways:
using a monochromatic beam and scanning the angle of incidence θ
using a polychromatic beam covering a range of q-values at any given θ
In practice, method 2 is useful a the range of q is measured simultaneously, which allows structural changes to be monitored as a function of time.

## Slide 92: Two possible methods for neutrons
Since q = 4πsinθ/λ, reflectivity R(q) can be measured in two ways:
using a monochromatic beam and scanning the angle of incidence θ (x-rays)
using a polychromatic beam covering a range of q-values at any given θ (neutrons)
In practice, method 2 is useful a the range of q is measured simultaneously, which allows structural changes to be monitored as a function of time.
When using polychromatic beam, the neutron wavelength distribution is determined from their time-of-flight, since the neutron velocity depends on their wavelength:
neutron velocity
time-of-flight distance
neutron wavelength

## Slide 93
DETECTOR IMAGE AT R=6x10-7
2-D DETECTOR
Efficient extraction of signal/noise
Off-specular studies
Salditt et al.

## Slide 94: Data reduction on for TOF NR
Reflectivity is presented as the ratio of reflected intensity to the incident beam:
below the critical q, IR/R0= 1 which is used for normalisation to an absolute scale
for a time-of-flight experiment, only 10% of the incident beam is reflected as above the critical angle the intensity falls with ~q-4
Io
IR x 10
I0/ IR
λc ~10.35 Å
log(I0/ IR)
qc ~0.0147 Å-1 (Si –D2O)
The critical q value is a property of the reflecting interface:
for silicon ρ1 = 2.07 x 10-6 Å-2
for D2O ρ2 = 6.35 x 10-6 Å-2
qc (Si-D2O) = 0.0147 Å-1
ρ2 > ρ1  total external reflection

## Slide 95: D17 – Time-of-flight and monochromatic vertical sample reflectometer at ILL
1 μm 10B on Si

## Slide 96: Angular resolution
Gaussian equivalent FWHM of angular spread after two slits:

## Slide 97
Monochromatization
Bragg-law:
Single crystal monochromators (silicon,diamond): Δλ/λ≈ 10-4
Pyrolytic graphite: Δλ/λ≈ 10-2
Intercalated pyrolytic graphite: Δλ/λ≈ 5*10-2
Darwin width
(dynamical theory):
Reflected Amplitude
(kinematic theory):
Illuminated
crystal volume
d
m

## Slide 98: Double Chopper set-up
Double Chopper transmission with chopper slit angle Φ0:
R. Cubitt and G. Fragneto, Appl. Phys. A 74 [Suppl.], S329– S331 (2002).
for
A. van Well, Physica B 80 & 81, 959– 961 (1992).
For zero opening:

## Slide 99
Dl/l | Disc Numbers | Disc separation (mm)
10 % | 1 & 4 | 800
8.8% | 2 & 4 | 700
4.2% | 1 & 3 | 350
3.0% | 2 & 3 | 250
5.4% | 3 & 4 | 450
1.2% | 1 & 2 | 100
Loose resolution allows high flux and measurements of thin films and liquid/liquid interfaces

## Slide 100: Double Chopper set-up
Wavelength resolution depends on:
Pulse length
Chopper opening variation
Beam width at chopper position
Active detector width
Time channel width
Binning
(for zero opening)

## Slide 101: 5. NR Data Analysis

## Slide 102
Planning a Reflectivity Measurement
• Simulation of reflectivity profiles is essential
– Can you see the effect you want to see?
– What is the best substrate? Which materials should be deuterated?
• If your sample involves free liquid surface you will need to use a reflectometer with a vertical scattering plane
If you want to follow a changes with time (kinetics) better to use a time-of-flight instrument.
• Preparing good (i.e. low surface roughness) samples is key
– Beware of large islands
• Layer thicknesses between 10 Å and 5000 Å
– But don’t mix extremes of thickness

## Slide 103: Data Analysis
Routine analysis of reflectivity data would ideally be solved by direct inversion of experimental data into either scattering length density, Nb(z), or even volume fraction, f(z), profiles.
Generally, this cannot be achieved due to the loss of phase information.
More than one model of Nb(z) may give the same reflectivity profile – phase information is lost
Measurement with multiple ‘contrasts’ normally resolves ambiguity
Physical knowledge of system may define a unique model
Contrast Variation

## Slide 105
_________________________________
Giovanna Fragneto HERCULES 2012
http://material.fysik.uu.se/Group_members/adrian/reflect.htm#Instruments
by Adrian Rennie (Uppsala University)
For a list of neutron reflectometers and programs to analyze the data:

## Slide 106: Practical Preparation (start at 13:30)
In order to reduce the raw data you will need LAMP (available for Windows,Linix and Mac): https://www.ill.eu/users/support-labs-infrastructure/software-scientific-tools/lamp/download-links/ Make sure that LAMP starts on your computer without errors. In order to fit the reflectivity curves you'll need a reflectivity fitting software. If you do not have one already then please download Motofit available for Windows and Mac (Version older than Catalina): https://www.wavemetrics.com/order/order_igordownloads.htm search for an older IgorPro Version if IgorPro8 does not work on your hardware and install it. Then download Motofit for the given IgorPro Version here: https://sourceforge.net/projects/motofit/ and install it. Please make sure that IgorPro starts and you see 'Motofit' in the menu bar. Then please download the raw data here: https://drive.google.com/file/d/1KL-pt-C-slLUr-Qx9AnND3_1i2Ko_lYG/view?usp=sharing and unzip it.

## Slide 107: Practical Demonstration
TOF data of a single layer on Si substrate:
Show spectrum of DB and RB
Number of angles: 3
IO -> choose correct file/output path
Reduce Data (RB:317370,317371,317372;DB:317369), click run look at it in PLOT
Make sure ascii .mft file was saved in the right folder
NOW: Calculate thickness
Check silicon SLD on NIST page
Fit data (thickness+density, which form of SiO2?), Add second layer? With Motofit

## Slide 108: Practical Groups 11 and 12
TOF data of a single layer (SiO2) on crystal silicon substrate:
Reduce Data (RB:53062,53063-63064,53065-53069;DB:53060) use san
NOW: Calculate thickness
Fit data (thickness+density, which form of SiO2?)
If time permits: TOF data of multilayer:
Reduce Data (RB:10627,10708;DB:10611) use dan (cycle 113)
Calculate bilayer thickness